Pos. 0	Acoustic wall and ceiling panels

Richter Acoustic-CompactBoard with MR 050 250 V micro-perforations.

Specifications:

front:	Micro-perforations at 0.5mm in diameter spaced at 2.5mm on center. Second

series of Micro Perforations set in between the first micro-perforations and offset 45 degrees resulting in the rows spaced at 1.25mm on center. The micro perforations are from edge to edge of the acoustic panel.

core:	Acoustically tuned MDF core with special drilling

back:	Balancing backer with acoustical fleece backing.

Finish option 1. Specifier to select preference.

finish:	front:		0.6mm HPL surface. Manufacturer:   ______________

Color/pattern:   ______________

edges:	ABS edgebanding to match HPL selection at 0.4mm to 2mm in thickness.

back:	Balancing backer for panel stability.

Finish option 2. Specifier to select preference.

finish:     front:		Grade A 0.5mm thick wood veneer laminated to 0.4mm thick CPL

carrier.

Veneer:   _________________

Veneer cut:   _________________

Veneer match:   _________________

Clear finished.

edges:	Wood veneer to match selected species of face veneer. 0.6mm to 2mm in thickness. Clear finished.

back:		0,4mm balancing CPL for panel stability and black acoustical fleece.

Primed only

Formats:

Width:	25mm up to 1550mm. Additional widths on request.

Length:	304mm up to 4000. Additional lengths on request.

Thickness:	17mm, 19mm. Optional thicknesses on request.