Pos. 0	Acoustic wall and ceiling panels

Richter Acoustic-CompactPanel slotted with SC 200090.

Specifications:

front:	Slotted with 2 mm (0.08”) groove, distance between grooves 9 mm (0.35”).

core:	Acoustically tuned MDF core with acoustic drilling on the back surface.

back:	Balancing backer with black acoustical fleece adhered to back..

Finish option 1. Specifier to select preference.

finish:	front:		Melamine/HPL surface. 		Manufacturer:   ______________

Color/pattern:   ______________

edges:	ABS edgebanding to match selection at 0.4mm to 2mm in thickness.

back:	Balancing backer for panel stability.

Finish option 2. Specifier to select preference.

finish:     front:		Grade A 0.5mm thick wood veneer

Veneer:   _________________

Veneer cut:   _________________

Veneer match:   _________________

Clear finished.

edges:	Wood veneer to match selected species of face veneer. 0.6mm to 2mm in thickness. Clear finished.

back:		0,5mm balancing veneer for panel stability , clear primed finish and

black acoustical fleece.

Formats:

Width:	100mm (3.93”) up to 1550mm. (61”)  Additional widths on request.

Length:	304mm (11.97”) up to 4000mm (157.48”). Additional lengths on request.

Thickness:	17mm (0.67”), 19mm (0.75”), 20mm (0.79”). Optional thicknesses on request.