Pos. 0	Acoustic wall and ceiling panels

Richter Acoustic-Lightboard® with MS 075 500H micro-perforations.

Specifications:

front:	Horizontal Micro-perforations at 0.75 mm in width and 5mm in length spaced at 5 mm in width and 10 mm in length on center.

The micro perforations have an unperforated border minimum 10 mm at all four edges.

core:	Acoustically tuned honeycomb core with a standard rigid perimeter frame at 25 mm or 50 mm in width.

back:	RU 0510 perforations. 5 mm diameter at 10 mm center to center. 50 mm un-perforated border at all four edges.

Finish option 1. Specifier to select preference.

finish:	front:		0.8 mm HPL surface. Manufacturer:   xxxxxxxxxxxxxxx

Color/pattern:   xxxxxxxxxxxxxxxx

edges:	ABS edgebanding to match HPL selection at 0.4 mm to 2 mm in thickness.

back:	HPL balancing sheet for panel stability.

Finish option 2. Specifier to select preference.

finish:     front:		Grade A 0.5 mm thick wood veneer laminated to 1.5 mm thick HDF

carrier.

Veneer:   xxxxxxxxxxxxxxxxxxxx

Veneer cut:   xxxxxxxxxxxxxxxxxxxx

Veneer match:   xxxxxxxxxxxxxxxxxxxxx

Clear finished.

edges:	Wood veneer to match selected species of face veneer. 0.6 mm to 2 mm in thickness.

Clear finished.

back:	Grade C balancing veneer laminated to 1.5 mm thick HDF carrier for panel stability.

Primed only.

Formats:

Width:	25 mm up to 1550 mm. Additional widths on request.

Length:	304 mm up to 4000 mm. Additional lengths on request.

Thickness:	16 mm, 19 mm. Optional thicknesses on request.