Pos. 0	Acoustic wall and ceiling panels

Richter Acoustic-Lightboard® with MR 075 500 V micro-perforations.

Specifications:

front:	Micro-perforations at 0.75mm in diameter spaced at 5mm on center. Second

series of Micro Perforations set in between the first micro-perforations and offset 45 degrees resulting in the rows spaced at 2.5mm on center. The micro perforations have an unperforated border minimum 10 mm at all four edges.

core:	Acoustically tuned honeycomb core with a rigid perimeter frame at 25mm or 50mm in width.

back:	RU 0510 perforations. 5mm diameter at 10mm center to center. 50mm un-perforated border at all four edges.

Finish option 1. Specifier to select preference.

finish:	front:		0.8mm HPL surface. Manufacturer:   xxxxxxxxxxxxxxx

Color/pattern:   xxxxxxxxxxxxxxxx

edges:	ABS edgebanding to match HPL selection at 0.4mm to 2mm in thickness.

back:	HPL balancing sheet for panel stability.

Finish option 2. Specifier to select preference.

finish:     front:		Grade A 0.5mm thick wood veneer laminated to 1.5mm thick HDF

carrier.

Veneer:   xxxxxxxxxxxxxxxxxxxx

Veneer cut:   xxxxxxxxxxxxxxxxxxxx

Veneer match:   xxxxxxxxxxxxxxxxxxxxx

Clear finished.

edges:	Wood veneer to match selected species of face veneer. 0.6mm to 2mm in thickness. Clear finished.

back:		Grade C balancing veneer for panel stability.

Primed only.

Formats:

Width:	25mm up to 1550mm. Additional widths on request.

Length:	304mm up to 4000. Additional lengths on request.

Thickness:	16mm, 19mm. Optional thicknesses on request.